Product Data Sheet

Product Code: FMPP-2180

Product Name: PP Filler Masterbatch

BLAU BATCH supplies high-performance calcium carbonate filler masterbatches for polyolefin polymers. Our advanced formulation delivers excellent CaCO₃ dispersion and high loading, optimizing performance, enhancing production efficiency, and reducing costs.

General Description

This product contains: CaCO3, resin and some additives. It’s suitable for applications such as woven sacks, raffia, injection molding, sheets, thermoforming, blown film, and non-woven fabrics.
Ideal where increased stiffness, improved processability, and reduced shrinkage are required without compromising basic mechanical performance.

# Physical Properties:

| Property | Value |
| --- | --- |
| Carrier | PPH |
| CaCO₃ | 80% ± 2% |
| Density @23 °C (Specific gravity) | 2.1 |
| MFI (2.16 kg/230 °C) | 8 g/10 min |
| Moisture content | < 0.05 |

# Technical Properties:

| Appearance (Surface color) | White |
| --- | --- |
| Additives | Dispersion agent, processing aid |
| Processing temperature (°C) | 160-250 |
| Expiry date | 6 months |
| Packing | 25 kgs per PP bag |
| Storage | Keep at dry condition. |

Method of Usage

Easy to disperse and homogeneous, Blau batch Filler Masterbatch can be directly added or pre-blended with resin using dosing units. It avoids contamination and ensures smooth processing.

Caution:

This product may absorb moisture after long-term storage or contact with a moist environment. Please dry it in a dryer before use.

This product information is based on our general experience and does not constitute a specification. Since many factors affect the use of our products, no warranty is given or implied with respect to this information or patent infringement. We do not accept liability for any loss or damage arising from the use of this information. All sales are subject to our Standard Terms and Conditions of Sale.